During an NDT (non-destructive testing) inspection, a crack is visually identified and located at stringer number 14 on the wing spar shear web.

Photos of the defect are provided; we are currently in contact with the manufacturer for a repair disposition.

No part numbers were provided. Take a second look at the above, last photo: taken through the bolt hole.

Part Total Time: 29,756 hours